Specification Clause for Ketley Brick Slips

Product size 215 x 65 x 15 mm 215 x 65 x 18 mm

Reverse key 2.5mm ribbed key for 15mm slip or 4.5mm dovetail (for precast concrete applications) for 18mm slip

Colour Staffordshire blue, Staffordshire brown brindle, Staffordshire red, Staffordshire light multi, Staffordshire dark multi, Staffordshire red blue

Maufacturing Extruded

Net dry density 2200kg/m3

Weight 15mm thick 0.45kg/slip & 18mm thick 0.57kg/slip

Texture Smooth, sanded or textured

Water absorption ≤4.5%

Performance class (to BS EN 771-1:2011)

Durability: F2, frost resistant.

Dimensional tolerance, mean: T2.

Dimensional tolerance, range: R1.

Reaction to fire: A1.

Soluble salt: S2.