Specification Clause for Ketley Class A Bricks

Product size 215 x 102.5 x 50mm, 215 x 102.5 x 65mm, 215 x 102.5 x 73mm

Colour Staffordshire blue, Staffordshire red, Staffordshire brown brindle, Staffordshire brown antique

Texture Smooth

Type Solid or perforated

Manufacture Extruded and wirecut

Performance class (to BS EN 771-1:2011)

Compressive strength ≥ 125MN/m²

Water absorption ≤ 4.5%

Engineering grade Class A

Initial rate of water absorption ≤ 1.5kg/m

Soluble salt content S2

Durability F2

Fire reaction A1

Dimensional tolerance mean T2

Dimensional tolerance range R1

Special shapes to BS4729 2005